ARCHITECTURAL SPECIFICATIONS FOR

CUBE CONTINUOUS SERIES 2

WOOD CEILING SYSTEM

[Project Name]

[Project Location]

PART 1 — GENERAL

1.1 Description of Work:

- Work Included: Provide Architectural Components Group, Inc. Cube Continuous Series 2 wood ceiling system where shown on architectural drawings, and as specified in this specification.

1.2 Quality Assurance:

- Architectural Components Group, Inc. Cube Continuous Series 2 CC2-xyyy wood ceiling products for this project shall maintain the quality as instituted by the architect or A.W.I.

- Design Criteria: Manufacture Cube Continuous Series 2 CC2-xyyy wood ceiling shall be installed true and plumb to within manufacturing tolerance of 1/8” within 8’ of length.

- Product Construction: Wood shall be kiln dried to 10%. Cracking, checking and warpage of members will not be acceptable.

1.3 Submittals:

- Technical Data: Submit manufacturer’s data and installation instructions.

- Shop Drawings: Submit 4 copies of shop drawings showing all areas involved, attachment conditions and perimeter circumstances.

- Submittal Samples: Submit 1 product sample for approval by architect.

1.4 DELIVERY, STORAGE AND HANDLING

- Material must be stored and installed only in secured ambient environment (humidity min. 35% -max. 55%, temperature not to exceed 86 deg.)

- Windows, Doors and all wet-work must be completed before un-packaging and installation. Handle carefully to avoid damaging.

PART 2 — PRODUCTS

2.1 Acceptable Manufacturer:

Architectural Components Group, Inc., 521 George Street, Marshfield, MO 65706
Phone (417) 869-6777	Fax (417) 869-7888

  - Product Type

- Product Configuration: ACGI Cube Continuous Series 2 wood system product: CC2-xyyy

Cube Continuous wood system shall be provided in:

Cube Continuous Series 2

Panel Width: 24” or 48”

Panel Length: 24”or 48”

Cell Size: 3”, 4”, 6”, 8” or 12” square

Cell Depth: 2”, 2-1/2”, 3”, 3-1/2” or 4”

Blade Thickness: 3/8”, 9/16”, 5/8”, 3/4” or custom thickness available.

Nomenclature for CC2-4200

CC2 = Cube Continuous Series 2

4 = 4” cell width

200 = 2” cell depth

- Main-runners shall be made from solid lumber with internal notches to support the cube panels. Main runners are suspended from the structure using 12 gauge hanger wires.  Cross runners are to be manufactured from solid lumber to stabilize the main runners and do not support the cube panels.

- Species and Grade: System shall consist of solid specie architectural grade lumber.

- Finish: Finish shall utilize ACGI clear finish with satin sheen or specify custom stain to match architect sample.

- Certification: The solid wood shall or shall not be FSC. If FSC, the Chain of Custody Certificate shall or shall not be provided.

- Fire Rating: Wood panels shall achieve a Class I(A) or Class III(C) fire rating.

- Attachment System: Cube Continuous wood ceiling system shall be suspended according to manufacturers suggested method of suspension as per the design details provided in the plans.

PART 3 -- EXECUTION

3.1 Installation

- The Cube Continuous wood ceiling system shall be handled and installed with care in order to prevent surface and structure damage. Field cutting shall be kept to a minimum and performed as recommended by manufacturer.

- The ceiling system shall be suspended by wood grid members spaced 48” on center. Cross members shall intersect every 48” on center. Each main runner shall be suspended with aircraft cable, suspended 48” end on end [oc.]

- Panels shall be installed by laying each panel or cross member into the wood grid. Each panel shall be secured in place as per the recommendation of the manufacturer, as detailed in submittal drawings.

PART — 4 WARRANTY

4.1 Product Warranty

- Architectural Components Group, Inc. shall warranty the Cube Continuous wood ceiling system against manufacturer’s defects up to one year. Changes in finish or dimensions due to ultra violet light, excessive temperature or humidity conditions [see 1.4.A above] and/or abuse of any kind shall void any warranties from ACGI.

- Install conditions for the area should remain for the proper occupied conditions of humidity and temperature (humidity min. 25% - max. 55%, temperature not to exceed 86 degrees).

- The contractor shall warranty for one year all work from final acceptance of completed work.

# Text boxes

Architectural Components Group, Inc.

521 George St.

Marshfield, MO 65706

417-869-6777  /  417-869-7888 fax

info@acgiwood.com  /  acgiwood.com