ARCHITECTURAL SPECIFICATIONS FOR

ENCORE™ SERIES 6 ACOUSTICAL WOOD

WALL AND CEILING PANELS

[Project Name]

[Project Location]

PART 1 — GENERAL

1.1 Description of Work:

- Work Included: Provide Architectural Components Group, Inc. Encore Series 6 EN6 wood ceiling and wall system where shown on architectural drawings, and as specified in this specification.

1.2 Quality Assurance:

- Architectural Components Group, Inc. Encore Series 6 ceiling and wall system for this project shall maintain the quality as instituted by the architect or A.W.I.

- Design Criteria: Manufacture of Encore EN6-xxxx-Cx ceiling and wall system shall be installed true and plumb to within manufacturing tolerance of 1/8” within 8’ of length.

- Product Construction: Wood shall be kiln dried to 10%. Cracking, checking and warpage of members will not be acceptable.

1.3 Submittals:

- Technical Data: Submit manufacturer’s data and installation instructions.

- Shop Drawings: Submit 4 copies of shop drawings showing all areas involved, attachment conditions and perimeter circumstances.

- Submittal Sample: Submit 1 product sample for approval by architect.

1.4 Delivery, Storage and Handling

- Material must be stored and installed only in secured ambient environment (humidity min. 25% - max. 55%, temperature not to exceed 86 degrees).

- Windows, doors and all wet-work must be completed before unpacking and installation. Handle carefully to avoid damage.

PART 2 — PRODUCTS

2.1 Acceptable Manufacturer

Architectural Components Group, Inc., 521 George Street, Marshfield, MO 65706
Phone (417) 869-6777	Fax (417) 869-7888

2.2 Product Type

- Product: Encore™ Series 6 acoustical wood system shall be product: EN6-xxxx-Cx

Nomenclature for EN6-4896-C10

EN6 = Encore™ Series 6

4896 = a panel 48” wide x 96” length

C = 3/4” thick substrate

10 = face grooves 10mm O.C.

- Size: Encore Series 6 panels shall be up to 5’ wide x 12’ length [limited by veneer length] x 3/4” thick.

- Face Profile: Face grooves shall be 8, 10, 12, 16 or 25mm on center.

- Specie: System shall consist of specie wood veneer [e.g., quartered, slip-matched cherry veneer].

- Finish: Finish shall utilize ACGI clear finish with satin sheen or specify custom stain to match architect sample.

- Core: The substrate material shall or shall not be manufactured with no added urea formaldehyde.

- Certification: The wood veneer shall or shall not be FSC. The substrate shall or shall not be FSC. If FSC, the Chain of Custody certificate shall or shall not be provided.

- Fire Rating: Wood panels shall achieve a Class I(A) or Class III(C) fire rating.

- Attachment System: Encore Series 6 ceiling and wall system shall be mounted according to manufacturers suggested method of suspension. This system shall comply with Seismic Zone 2-4 regulations as required.

PART 3 — EXECUTION

3.1 Installation

- The Encore ceiling and wall system shall be handled and installed with care in order to prevent surface and structure damage. Field cutting shall be kept to a minimum and performed as recommended by manufacturer.

- The contractor shall measure ceiling and/or wall areas to establish layout for hangers and carriers, in accordance with installation instructions.

- Ceiling panels shall be suspended using ACGI FP1, FP2, FP3, FP4, FP5 or FP6 mounting methods.

- Contractor shall clean all panels prior to installation according to manufacturer’s recommended maintenance procedures. Upon completion of installation, panels shall be inspected and cleaned as needed.

PART 4 — WARRANTY

4.1 Product Warranty

- Architectural Components Group, Inc. shall warranty the Encore acoustical wood panel system against manufacturer’s defects up to one year. Changes in finish or dimensions due to ultra violet light, excessive temperature or humidity conditions and/or abuse of any kind shall void any warranties from ACGI.

- Install conditions for the area should remain for the proper occupied conditions of humidity and temperature (humidity min. 25% - max. 55%, temperature not to exceed 86 degrees).

- The contractor shall warranty for one year all work from final acceptance of completed work.

# Text boxes

Architectural Components Group, Inc.

521 George St.

Marshfield, MO 65706

417-869-6777  /  417-869-7888 fax

info@acgiwood.com / acgiwood.com