Architectural Components Group, Inc.

521 George St.

Marshfield, MO 65706

417-869-6777  /  417-869-7888 fax

info@acgiwood.com / acgiwood.com

ARCHITECTURAL SPECIFICATIONS FOR

WOOD BEAM SERIES 1

CEILING or WALL SYSTEM

[Project Name]

[Project Location]

PART 1 - GENERAL

1.1 Description of Work:

- Work Included: Provide Architectural Components Group, Inc. Wood Beam Ceiling or Wall System where shown on architectural drawings, and as specified in this specification.

1.2 Quality Assurance:

- Architectural Components Group, Inc. BM1-xyx Wood Beam System for this project shall maintain the quality as instituted by the architect or A.W.I.

- Design Criteria: Manufacture of BM1-xyx Wood Beam shall be installed true and plumb to within manufacturing tolerance of 1/8” within 8’ of length.

- Product Construction: Wood shall be kiln dried to 10%. Cracking, checking and warpage of members will not be acceptable.

1.3 Submittals:

- Technical Data: Submit manufacturer’s data and installation instructions.

- Shop Drawings: Submit 4 copies of shop drawings showing all areas involved, attachment conditions and perimeter circumstances.

- Submittal Samples: Submit 1 product sample for approval by architect.

1.4 Delivery, Storage and Handling

- Material must be stored and installed only in secured ambient environment (humidity min. 35% - max. 55%, temperature not to exceed 86 deg.)

- Windows, doors and all wet-work must be completed before unpacking and installation. Handle carefully to avoid damage.

PART 2 — PRODUCTS

2.1 Acceptable Manufacturer

Architectural Components Group, Inc.,  521 George St., Marshfield, MO 65706

Telephone (417) 869-6777	Fax (417) 869-7888

2.2 Product Type

- Product Configuration: Wood Beam system, product # BM1-xyx Wood Beams shall be provided in a size of x” deep y” wide x” deep.

Nomenclature for BM1-646-C:

BM1 = Beam Series 1

646 = a three-sided beam that is 6” tall x 4” wide x 6” tall

C = 3/4” thick substrate

- Species: System shall consist of desired wood veneer species [e.g., cherry plain-sliced, book-matched]; laminate; or paint.

- Finish: Wood veneer finish shall utilize ACGI clear finish with satin sheen or specify custom stain to match architect sample.

- Certification: Wood veneer shall or shall not be FSC certified. The core material shall or shall not be FSC certified. If FSC, Chain of Custody shall or shall not be provided.

- Substrate material shall or shall not be manufactured with no added urea formaldehyde.

- Attachment System: Wood Beam shall be suspended according to manufacturers suggested method of suspension as per the design details provided in the plans.

- Fire Rating: Wood Beams shall be constructed with components achieving a Class A (flame spread <25, smoke developed <450) rating.

PART 3 — EXECUTION

3.1 Installation

- Wood Beam System shall be handled and installed with care in order to prevent surface and structure damage. Field cutting shall be kept to a minimum and performed as recommended by manufacturer.

- The Wood Beam ceiling system shall be suspended by threaded rod on 4’ centers according to manufacturers suggested layout instructions.

- Beams shall be installed by screwing each suspension plate into the internal structure of the wood beam.

PART 4 — WARRANTY

4.1 Product Warranty

- Architectural Components Group, Inc. shall warranty the Wood Beam System against manufacturer’s defects up to one year. Changes in finish or dimensions due to ultra violet light, excessive temperature or humidity conditions [see 1.4.A above] and/or abuse of any kind shall void any warranties from ACGI.

- Install conditions for the area should remain for the proper occupied conditions of humidity and temperature (humidity min. 25% - max. 55%, temperature not to exceed 86 degrees).

- The contractor shall warranty for one year all work from final acceptance of completed work.